# Resistivity measurement of an Aluminium thin film in linear geometry (2-probe & 4-probe)

### Aim

To measure the electrical resistance and determine the resistivity of an Aluminium (Al) thin film using linear 2-probe and 4-probe measurement techniques, and to demonstrate the elimination of contact resistance using the 4-probe method.

Figure : Aluminium Thin film sample on puck with linear contacts

### Apparatus

- Thin Film Sample: Aluminium thin film deposited on an insulating substrate with a linear array of metallic contacts.

- Constant Current Source: Capable of sweeping current in the microampere (μA) to milliampere (mA) range.

- Digital Voltmeter: High input impedance voltmeter (or a combined Source Measure Unit).

- Connecting Leads & Probes: For establishing electrical contact with the film.

- Thickness Measurement Tool: Profilometer or optical interferometer to measure the film thickness (t).

### Theory

When measuring the resistance of highly conductive materials like Aluminium thin films, the resistance of the sample is often very small, making the measurement technique critical.

1. The 2-Probe Method:

In a 2-probe setup, the same two probes are used to both inject the current (I) and measure the resulting voltage drop (V). The resistance calculated using Ohm's Law (R = V/I) is the total system resistance, which includes:

R_measured = R_sample + 2R_contact + 2R_lead

Because the contact resistance (R_contact) and lead resistance (R_lead) are often much larger than the resistance of the Al thin film itself, the 2-probe method inherently overestimates the true sample resistance.

2. The 4-Probe Method (Linear Geometry):

To accurately measure the true resistance of the thin film, a linear 4-probe setup is used. Four equally spaced probes are placed in a line across the sample:

- Current (I) is injected through the two outer probes.

- The voltage drop (V) is measured across the two inner probes.

Because the voltmeter has a very high input impedance, practically zero current flows through the inner voltage leads. Consequently, there is no voltage drop across the inner contact points or leads, eliminating R_{contact} and R_{lead} from the measurement. The measured voltage corresponds strictly to the resistance of the thin film material between the inner probes.

Resistivity Calculation:

For a thin film (where thickness t is much less than the probe spacing s) on a semi-infinite plane, the sheet resistance (R_s) and volume resistivity (ρ) are given by:

R_s = (π / ln(2)) * (V / I)

ρ = R_s * t

### Procedure

Part A: 2-Probe Measurement

- Connect the current source to two adjacent probes on the sample.

- Connect the voltmeter in parallel across the exact same two probes.

- Sweep the source current across a predefined range (e.g., 2 μA to 10 μA).

- Record the corresponding voltage values.

- Plot a graph of Voltage vs. Current. The slope of this linear fit represents the total resistance (R_2-probe).

Part B: 4-Probe Measurement

- Connect the current source to the outer two probes (Probes 1 and 4).

- Connect the high-impedance voltmeter to the inner two probes (Probes 2 and 3).

- Sweep the source current across a predefined range (e.g., 1 mA to 5 mA).

- Record the corresponding voltage values across the inner probes.

- Plot a graph of Voltage vs. Current. The slope of this linear fit represents the true sample resistance (R = V/I).

- Calculate the sheet resistance (R_s) using the geometric correction factor π/ln(2).

- Multiply by the film thickness (t) to find the final resistivity (ρ).

### Observations & Calculations

Figure : Plots summarising the resistivity calculations

2-Probe Data

| V_2p (mV) | I_2p (μA) | I_err_2p (μA) |
| --- | --- | --- |
| 0.4 | 2.006 | 0.024 |
| 0.8 | 4.713 | 0.007 |
| 1.0 | 5.161 | 0.007 |
| 1.5 | 8.316 | 0.041 |

4-Probe Data

| I_4p (mA) | V_4p (mV) | V_err_4p (mV) |
| --- | --- | --- |
| 1 | 0.4596 | 0.0002 |
| 2 | 0.9118 | 0.0002 |
| 3 | 1.3650 | 0.0007 |

### Results

2-probe

- Calculated Resistance (R): 175.81 Ω

- Standard Error: ±13.68 Ω

4-probe

- Calculated Resistance (R): 0.4527 Ω

- Standard Error: ±0.0003 Ω

### Precautions

- Gentle Contact: Probes should be placed gently on the thin film to avoid scratching, puncturing, or damaging the Aluminium layer.

- Ohmic Contacts: Ensure the contacts are ohmic (linear V-I relationship) rather than rectifying. The V-I plots should be perfectly straight lines.

- Thermal Effects: Keep the current relatively low to prevent Joule heating, which alters the intrinsic resistivity of the Aluminium.

- Edge Effects: For the standard geometric correction factor (π/ln(2)) to be valid, the probes must be placed near the center of the sample, far away from the sample boundaries.